## CONCRETE SIDEWALK.

(REV 9-17-09) (1-13)

ARTICLE 522-1 (page 678) the text is deleted and the following substituted:

Construction, reconstruction or removal of concrete sidewalk and curb cut ramps, will in accordance with these specifications, and in conformity with the lines, grades, dimensions and notes shown in the plans and/or current edition of the Department’s Design Standards.

ARTICLE 522-2 (page 678) is expanded by the addition of the following paragraph:

Assume all risk when placing concrete under adverse weather conditions, and permission from the Engineer to place concrete under such conditions will in no way relieve the Contractor of the responsibility of satisfactory results.

ARTICLE 522-4 (page 678) is expanded by the following:

Excavation or fill to the required grade or to match existing conditions. Compact the foundation material upon which the sidewalk is set to a firm even surface, true to grade and cross section. Place the concrete on moist foundation material.

ARTICLE 522-7 (page 678) is expanded by the addition of the following new Subarticles:

522-7.3 Repair of Minor Defects:  Remove the forms within 24 hours after the concrete has been placed, and fill minor defects with mortar composed of one part portland cement and two parts fine aggregate.  Plastering will not be permitted on the surface of the sidewalk.  Remove and replace any rejected sidewalk without additional compensation.

522-7.4 Sidewalk Removal: Remove existing sidewalk in accordance with Article 110-7.

522-7.5 Clean-up: Remove from the job site any surplus or discarded materials or rubbish and restore the job site area to a condition acceptable to the Department, upon completion of work, and before final payment is made.

ARTICLE 522-8 (page 679) is expanded by the following new paragraph:

After the concrete has set sufficiently, but no later than 72 hours after placing, refill the spaces in back and in front of the sidewalk to the required elevation with suitable material, compacting in layers not thicker than six inches.

ARTICLE 522-9 (page 679) is expanded by the following:

Curb ramps built, as part of the construction of a concrete sidewalk will be paid for as a part of the area in square yards of concrete sidewalk constructed.  Curb ramps built after construction (retrofit), as separate structures will be paid for as each under Item No. E522-74 Curb Ramp (Retrofit).

ARTICLE 522-10 (page 679) is expanded by the following:

Payment for removal and disposal of existing sidewalk will be governed by Section 110.

Payment will be made under the items specified in the Bid Price Proposal.