“Use on Manufacturer’s Letterhead”

# MATERIAL CERTIFICATION

Florida D.O.T.

TYPE___GROUND TIRE RUBBER FOR USE IN ASPHALT RUBBER BINDER

Specification Number (919)

APL Product Identifier Number:

Approved Material Name:

Batch or LOT Number:

Manufacturer:

Customer Name:

Delivery Location/Address:

D.O.T.  Project Number (if known):

Contract Number (if known):

_____________________________________________________________________________ Physical/Chemical Properties of Ground Tire Rubber (specified in F.D.O.T.  Section 919)

1. Specific Gravity: ________________________________________________________(1.02 to 1.20)

2. Moisture Content (%):____________________________________________________(Maximum 0.75%)

3. Metal Contaminants (%): __________________________________________________(Maximum 0.01%)

4. Gradation (% Passing No. 30 sieve): _________________________________________(Minimum 98%)

5. Acetone Extract (%):_____________________________________________________(Maximum 25%)

6. Rubber Hydrocarbon Content (%): __________________________________________(40% to 60%)

7. Ash Content (%): ________________________________________________________(Maximum 8%)

8. Carbon Black Content (%): ________________________________________________(20% to 40%)

9. Natural Rubber (%): _____________________________________________________(16% to 45%)

We certify that the above listed product is the same product approved by the Florida D.O.T. and meets the requirements of section 919 of the Contract Specifications (Ground Tire Rubber for Use in Asphalt Rubber Binder).

Manufacturer Officer or Designee________________________

Signature:________________________________

Date:____________________________________

(Notarized)