## removal of existing thermoplastic traffic stripes and/or markings.

(REV 9-22-09) (1-13)

PAGE 856. The following is a new Section added at the end of Section:

SECTION ME711-70
REMOVAL OF EXISTING THERMOPLASTIC
TRAFFIC STRIPES AND/OR MARKINGS

ME711-70.1 Description.

Remove existing thermoplastic traffic stripes and/or markings from pavement surfaces.

ME711-70.2 Removal Requirements.

Remove existing pavement marking by water blasting, grinding, sandblasting, or other method approved by the Engineer. Do not use chemicals for the removal of thermoplastic traffic stripes and/or markings.

Provide positive means to control dust and accumulation of debris from the removal operations. Remove all pavement marking materials from the pavement surface. Remove accumulated piles of any debris as a result of the removal operation from the right of way and dispose of in accordance with applicable Federal, State, and Local regulations, at no additional cost to the Department.

Apply a new thermoplastic traffic stripes and/or markings meeting the requirements of Section 711 before the end of the workday.

ME711-70.3 Protection of Existing Pavement Surfaces.

Conduct removal operations in a manner that will not damage existing pavement surfaces (concrete or asphalt) or damage pavement joint materials. Repair, to the satisfaction of the Engineer, any damage as a result of the removal operations.

Do not paint over existing pavement markings to blackout, hide, or disguise markings.

ME711-70.4 Method of Measurement.

The quantities to be paid for will be the area, in square feet, of existing thermoplastic traffic stripes and/or markings removed and accepted.

ME711-70.5 Basis of Payment.

Price and payment will be full compensation for all work specified and will include the removal of thermoplastic traffic stripes and/or markings, furnishing all tools, machines, equipment, and incidentals necessary to complete the work.

Payment will be made under the items specified in the Bid Price Proposal.