HOT BITUMINOUS MIXTURES - ACCEPTANCE PROCEDURES.

(REV 9-5-00) (1-01)

SUBARTICLE 330-2.1.3 (of the Supplemental Specifications) is deleted and the following substituted:



330-2.1.3 Referee System: The Department has established a referee system to verify the validity of the acceptance test results on LOTs at the asphalt plant. The Department will evaluate the acceptance test results with data from split samples run by the District and Central Labs. The Engineer will make a final determination and disposition of the acceptance test results. Acceptance results will be considered non-representative if the test results from the Field and Referee samples differ by more than 0.56 for asphalt content (regardless of the test method) or by more than the allowable difference obtained from Figure 2 of FM 1-T 030. When the referee analysis indicates that one or more test results are not representative, the Engineer will discard the non-representative test value(s) and base payment calculations for the LOT (including the sublot with the non-representative test values) on the remaining sublot(s) test data as defined in 331-5.

