9750900

Jobs with structures


975
STRUCTURAL COATING MATERIALS.


(REV 7-17-06) (FA 11-13-07) (7-08)
SECTION 975 (of the Supplemental Specifications) is expanded by the following new Article:
975-9 Anti-Graffiti Coating Materials.


975-9.1 General Requirements: Anti-graffiti coatings intended for use under this specification shall be of a composition to be capable of preventing the adhesion of graffiti and/or facilitating the removal of graffiti. All anti-graffiti coatings must possess the physical and handling characteristics that are compatible with the requirements of Section 563.


Anti-graffiti coatings shall contain less than [5.0 lb/gal]volatile organic compounds (VOC) as defined by 40 CFR Part 59, Subpart D.



The manufacturer will supply the following additional information:




a. Cleaning instructions and materials, as applicable. Surfaces must be cleanable with nonproprietary cleaners as defined in ASTM D6578.




b. Sacrificial Coating Removal instructions, as applicable.




c. Recommended base coat, as applicable.




d. Identification of coating system and type, as applicable.




e. Clear coats must contain a UV degradable color for inspection purposes. UV degradable color must dissipate in a reasonable time period to allow inspection but not detract from visual impact of the structure.

975-9.2 Material Tests: Meet the following requirements:
	Additional Laboratory Performance and Tests

	Test
	Method
	Limits

	Cyclic Weather Testing
	AASHTO R-31
	No blistering, cracking, checking, chalking, or delamination; color change less than 3 Delta E CIE LAB units; Retention of 60o Gloss ratio >= 0.80 

	Abrasion Resistance
	ASTM D968, 1,000 liters of sand
	No loss of coating thickness per ASTM D1005

	Impact Resistance
	ASTM D2794
	Minimum of 30 inch-pounds

	Graffiti Resistance
	ASTM D6578, Use identified marking materials; initial and recleanability; and after exposure initial and recleanability
	Cleanability Level 1, 2, or 3.

	Sacrificial Coating removability
	Per Manufacturer’s specifications: 6 months exposure at FDOT test site
	Complete removal of material from substrate

	MEK Double Rub
	ASTM D 5402; 50 rubs
	No coating wear through (4 minimum rating)

	Fluid Resistance
	ASTM D1308; Paint Thinner,

Gasoline
	No blistering, discoloration, softening or adhesion loss.


